FLUORESCENT BRIGHTENER 230

C.I.NO.: 230

Appearence: Light yellow powder

Moisture: 0.5%max

Insoluble in water: 0.5%max

Dyeing degree: 0.4%max

Fluorescent whitening strength: 100% (Compare to the standard)

Finess (sieved reside through 80 mesh) : 10%max

Uses: Mainly used to whiten cotton fabrics ^ capron fabrics and pulp,

and also used to increase brightness of lightcolored fabrics.

Packing: Iron drum lined with plastic bag,net weight 25 kg per drums.