FLUORESCENT BRIGHTENER 31

C.I.NO.: 31

Appearence: Light yellow homogeneous powder

Moisture: 5%max

Insoluble in water: 0.5%max

Dying degree: 0.4%min

Fluorescent whitening strenght: 100% (compared to standard )

Finess (sieved residue through 80 mesh) : 10%max

Uses: Mainly used for brightening of washing powder, soap paper and

artificial cotton^ nylon^ silk^ wool, etc.

Packing: Iron drum lined with plastic bag 25kg per drum.