FLUORESCENT BRIGHTENER BA

C.I.NO.: 113

Appearence: Light yellow powder

Moisture: 5%max

Dying degree: 0.4%min

Fluorescent whitening strength: 100% (Compare to the standard)

Insoluble in water: 10%max

Uses: Mainly used to whiten cotton fabrics ^ capron fabrics and pulp,

and also used to increase brightness of lighcolored fabrics. Packing: Iron drum lined with plastic bag» net weight 25kg per drums