FLUORESCENT BRIGHTENER BBU

C.I.NO.: 220

Appearence: Light yellow powder

Moisture: 5%max

Insoluble in water: 0.5%max

Dyeing degeree: 0.4%min

Fluorescent whitening strength: 100% (Compare to the standard)

Finess (sieved residue through 80 mesh) : 10%max

Uses: Mainly used to whiten cotton fabrics? capron fabrics and pulp,

and also to increase brightness of lighcolored fabrics. Packing: Iron drum lined with plastic bag,net weight 25kg per drums.