FLUORESCENT BRIGHTENER CBS-127

Structural formula:

C.I.NO.: 359

Appearance: Light yellow crystal powder

Melting point: 216 -222 C

Assay: 99%min

Loss on drying: 0.5%max

Ash content: 0.1%max

Uses: Widely used in the process of plastic^ syndetergen^ artificial

fabric, also can be used in printing. Packing: 20kg paper drum lined with plastic bag.