FLUORESCENT BRIGHTENER KCB

C.I.NO.: 367

Appearence: yellow green crystal

Shade: Similar to the standard sample

Solid content: 99.5%min

Melting Point: 210-212°C

Finess: Through 100 mesh.

Uses: Used to whiten synthetic cellulose fabric, plastic, plastic sheet,

press moulded material, polyester fabric, dyestuff and natural

paint coating.

Packing: Packed in bicorru gated paper case, lined with plastic bag, 10kg net weight each.