FLUORESCENT BRIGHTENER OB-1

C.I.NO.: 398-1

Appearence: yellow crystal powder

Solid content: 99.5%MIN

Melting Point: 351-353°C

Finess: Through 120 mesh.

Uses: Used to whiten original polyester liquid. Especial for increasing

whiteness of dacron fibre cottony fabric blending, and plastic products.

Packing: Packed in bicorrugated paper case,lined with plastic bag, 10kg net weight each.