FLUORESCENT BRIGHTENER OB

C.I.NO.: 184

Appearence: yellow green crystal powder

Solid content: 99.5%min

Melting point: 196-203°C

Shade: Similar to the standard sample

Finess: Through 100 mesh

Uses: Used to whiten thermoplastics materials PE^ PP^ PS^ ABS^

SAN^ SB^ CA> PA^ PMMA^ decron fibrk^ oil varnish^ paints

and paper.

Packing: Packed in bicorrugated paper case, lined with plastic bag, 10kg net weight each.