FLUORESCENT BRIGHTENER PB/EBF

C.I.NO.: 185

Appearence: light yellow crystal powder

Shade: Similar to the standard sample

Solid content: 99.5%min

Melting point: 216-220C

Finess: Through 100 mesh

Uses: Used to whiten varitious of polyene plastics, engineering ABS

plastics.

Packing: Packed in bicorrugated paper case, lined with plastic bag, 10kg net weight sach.