FLUORESCENT BRIGHTENER PBL

C.I.NO.: 216

Appearence: Light yellow or white powder

Insoluble in water: 0.5%max

Moisture: 5%max

Shade: similar to standard

Dying degree: 0.5%min

Fluorescent whitening strength: 100% (Compare to the standard)

Finess (sieved residue through 180 mesh) : 10%max

Uses: Mainly used to whiten white fibre, paper and lightn colorded fibre.

Also used to whiten material in discharging printing. Packing: Iron drum lined with plastic bag,net weight 25kg per drums