FLUORESCENT BRIGHTENER VBU

Structural formula:

C.I.NO.: 87

Appearence: Light yellow powder

Insoluble in water: 0.5%max

Moisture: 5%max

Shade: similar to standard

Dying degree: 0.5%min

Fluorescent whitening strength: 100% (Compare to the standard)

Finess (sieved residue through 80 mesh ) : 10%max

Uses: Mainly used to whiten cotton fabrics ^ capron fabrics and pulp,

and also used to increase brightness of lighcolored fabrics.

Packing: Iron drum lined with plastic bag» net weight 25kg per drums